## Slide 1: Radiation Test –Raspberry Pi Zero-
Noritsuna Imamura
noritsuna@siprop.org

## Slide 2: Purpose
Testing Total Dose for Raspberry PI Zero
  Target Devices
    Raspberry PI Zero: Ver.1.2
    MicroSD Card: TOSHIBA 8GB Class10(TOSHIBA MSDAR40N08G)

## Slide 3: Regulation
Target Radiation Dose
  ISS(International Space Station) Orbit
    SSP 30512 Revision C from NASA
  Heat Sink： 0.5[mm] Thickness of Aluminum Plate
    8773[rad/year] = 87.73 [gray/year]
  Mission Period: 2.6[year]
    87.73[gray/year] * 2.6[year] = 228.10 [gray]
Testing Radiation Dose
  Radioactivity: Cobalt-60
  Distance of the Radioactivity: 80[cm]
  Testing Date: 22/Mar/2017
  Irradiation Time: 5[h]
    46[ray/h] * 5[h] = 230 [gray]

## Slide 4: Calculation Tables
Table１．SSP 30512 Revision C
Table2．Dose Rate

## Slide 5: Test Method
Phase | No. | Task
Before Test | 1 | Setup Raspberry PI Zero, Consumption Current Logger, Power Supply.
 | 2 | Set Current Date on Raspberry PI Zero.
 | 3 | Run the Testing Application on Raspberry PI Zero.
During Test | 4 | Get CPU’s Temperature & Current Time in Every Minute.
 | 5 | Create Current Time as File and Write Current Temperature in this File.
 | 6 | Get & Save Current Consumption Current by Logger.

## Slide 6: Test Application 1/2
Check Targets & Reason
  CPU
    Raspberry PI Zero’s parts are a CPU & a voltage regulator only.
  Clock
    The clock shifts by a radioactive noise.
  MicroSD Card
    MicroSD Card has a micro computer.
    NAND Flash is weak in radiation.

## Slide 7: Test Application 2/2
#!/usr/bin/python
#coding:utf-8
import os
import commands
import datetime
import locale
d = datetime.datetime.today()
temp = commands.getoutput("vcgencmd measure_temp").split('=')
date_form_body=d.strftime("%Y-%m-%d %H:%M:%S ")
s=date_form_body + temp[1] + '\n'
date_form_file=d.strftime("%Y-%m-%d_%H:%M:%S")
filename=date_form_file + '.log'
f = open(filename,'a')
f.write(s)
f.close()
Operations
  Get CPU’s Temperature
  Get Current Time
  Create File by Current Time
  Write CPU’s Temperature & Current Time in this File.
  Close the File
  Exit the Application
  Run this Appli Every Minute by cron

## Slide 8: Consumption Current Logger
Reason
  Consumption current goes up by total dose degradation.
Operation
  Get & Save Current Consumption Current Every 30 seconds.

## Slide 9: Test Environment
Top: Upper-Surface Figure, Lower Left: Front Figure, Lower Right: Rear Figure
  Red Circle: Raspberry PI Zero
  Blue Circle: Irradiation Point

## Slide 10: During Test
The value of radioisotope, and an inside situation

## Slide 11: Test Result: CPU Temperature
Check Point | Check Target | Result | Success / Failure
Are the files made for every minute? | MicroSD Card | The files were created with the error for 1 second every minute. | Success
Were the files for 5 hours of test time made? | Clock | Just files existed. (Last – First) timestamps = 0:02. | Success
Isn't there any inaccurate temperature data? | CPU | Almost all the data was 25.0[C]. Occasional the data is 24.5[C]-26.0 [C]. | Success
By the above-mentioned test result, I judged that Raspberry PI Zero passed this test.

## Slide 12: Test Result: Consumption Current
Chart: Irradiation Time (min, 0=Start Time, 300=End Time)
By the above-mentioned test result, I judged that Raspberry PI Zero passed this test.
  But Consumption Current is increasing after 230min. It will be expected that radiation breaks if it is longer time.

## Slide 13: Test Result: Conclusion
By these test results, I judged that Raspberry PI Zero had radiation resistivity.
  It will be expected that radiation breaks if it is longer time.